[image: image6.jpg]ICONIC MEETINGS

..... Meet Influential People.....






Compression and energy absorption behavior of microwave sintered medium entropy alloy reinforced Magnesium matrix composite foam

Priyabrata Das 1*, Pulak Mohan Pandey 1
1 Department of Mechanical Engineering, IIT Delhi, New Delhi, India

*Presenting author
The present study incorporates sintering dissolution process to prepare a medium entropy alloy (MEA) reinforced Magnesium foam using carbamide particles as space holder for energy absorption application. A refractory BCC MEA (TiMoNb) prealloyed powder was fabricated through mechanical alloying route and used as the reinforcement in Mg matrix in order to achieve better mechanical properties. The TiMoNb prealloyed powder showed the presence of a single-phase BCC solid solution along with some minor peaks of Ti. The carbamide particles were removed through sintering dissolution process at a temperature of 300[image: image2.png]°C



 followed by final sintering of the green foam using microwave sintering at 550[image: image4.png]°C



 for 15 minutes with a high heating rate of 20K/min. Further, the homogeneous mixing of TiMoNb reinforcement in Mg matrix was confirmed by XRD phase analysis and EDX color mapping. The reinforcement content was varied from 0 weight percent (wt %) to 10 wt % while keeping the porosity of foam within the range of 33-38 % to capture its effect on mechanical response of composite foam. With the increase in the wt % of reinforced MEA, the compressive strength improved significantly owing to particle strengthening and grain refinement. The optimum combination of strength and energy absorption was obtained at 7.5 wt % reinforcement owing to the excellent interfacial bonding which facilitated effective load transfer mechanism. Incorporation of 7.5 wt% MEA reinforcement improved the peak strength and energy absorption by 81.6% and 159.3% respectively as compared to the pure Mg foam. 

Biography:
Priyabrata Das is currently pursuing his doctoral research at Indian Institute of Technology Delhi in the area of multi principal element alloy (MPEA) design and fabrication. His doctoral thesis work involves development of Mg based MPEA for biomedical application. Prior to joining IIT Delhi, he has completed his M. Tech. degree in Metallurgical and Materials Engineering from the Indian Institute of Technology Bhubaneswar in 2020 with an academic excellence award. He has published five peer reviewed papers in international journals.
Presenting author details 
[image: image5.png]


                                                                                       

Full name : Priyabrata Das
Mobile Number  / Whatsap Number: (+91)-7008867201
Twitter account : N.A
Linked In account : linkedin.com/in/priyabrata-das-565300189
Session name/ number : Polymers, Ceramics, and Composites
Category: Oral presentation

Date of Birth : 15th May 1996 (15/05/1996)
5 Recent Publications 
P. Das et al. "Corrosion, stress corrosion cracking and corrosion fatigue behavior of Magnesium alloy bioimplants", Corrosion Reviews, vol. 40, no. 4, 2022, pp. 289-333.

P. Das et al. "A review on corrosion properties of high entropy alloys fabricated by additive manufacturing", Transaction of Indian Institute of Metals, vol. 75, 2022, pp. 2465-2476.

P. Das et al. "Combined Effect of Sodium Lauryl Sulphate and Saccharin on Microstructure and Corrosion Performance of Electrodeposited Nickel Prepared from Modified Watts Bath", Metall Mater Trans A, vol. 52, 2021, pp. 1913–1926.

N. Rai, P. Das, and S. Gollapudi. "Can an amorphous alloy crystallize into a high entropy alloy?." Modelling and Simulation in Materials Science and Engineering, vol. 30, no. 2, 2021, p. 025007.

P. Das et al. "Evaluating the effect of grain size distribution on thermal conductivity of thermoelectric materials", Nano Express, vol. 1, no. 2, 2020, p. 020036.

[image: image6.jpg]